## Slide 1
EN 204
Material Science for Energy Applications
Class 8
Shaibal K Sarkar
Department of Energy Science and Engineering
shaibal.sarkar@iitb.ac.in

## Slide 2
Recap of the Objective
Understanding J = n.q.v
What is n ?
What is v ?
n = f (density of states, statistical distribution)
Density of states = f (band structure)
Band structure = f(periodic potential)
✓
✓

## Slide 3
What we have learned in the last class?
Electron concentration in conduction band
Hole concentration in valance band
f (E)
1 - f(E)
E
1
EF
What type of semiconductor it is?

## Slide 4
Ec
EF
Ev
N(E)
f(E)
Carrier Conc.
N-type
n0
Ec
EF
Ev
N(E)
f(E)
Carrier Conc.
P-type
Fermi Level, Population Density and Charge Carrier Distribution

## Slide 5
Electron Concentration

## Slide 6
Effective Density of States

## Slide 7
Law of Mass Action

## Slide 8
Fermi Level of Intrinsic Semiconductors
Position of the Fermi Level

## Slide 9
On similar note one can derive
Extrinsic carrier concentrations in terms of intrinsic carrier conc.
Charge Carrier Concentration

## Slide 10
Ec
EF
Ev
N(E)
f(E)
Carrier Conc.
N-type
n0
Ec
EF
Ev
N(E)
f(E)
Carrier Conc.
P-type
Fermi Level, Population Density and Charge Carrier Distribution

## Slide 11
Donor and Acceptor in Host Materials
The number of donor atoms is much smaller compared to host atoms. Therefore, the electrons from one donor atom can go to the other donor atoms only via the conduction /valence bands of the host crystal. Just like a Hydrogen atom, it is possible to have multiple localized level for a given atom (see the blue levels).
Good donors live close to the conduction band, so that they can offer electrons easily.
However, if they are below the midgap, the donor levels are marked with (D) to differentiate them from acceptor atoms (live close to the valence band).
In either case the material will be charge nutral

## Slide 12
Donor and Acceptor levels

## Slide 13
Amphoteric Dopants

## Slide 14
Donor and Acceptor statistics
What is the difference between ND and ND+ ?

## Slide 15
Donor Atoms in H2 atom analogy

## Slide 16
Recap : Hydrogen Atom
Equating both the forces: Coulomb force and Centrifugal force

## Slide 17
Donor Atoms in Real and Energy Space

## Slide 18
Donor Atoms in Real and Energy Space

## Slide 19
Localized vs. Delocalized states
2N states

## Slide 20
2N-2 states
Localized vs. Delocalized states

## Slide 21
Heavy Doping – Band-tail states